## Slide 1
Figures for
Slide dimension adjusted to fit A4
Figure typeface : helvetica

## Slide 3
Near-field
speckle #1
Near-field
speckle #2
Near-field
speckle #3
2D intensity profiles,
(measured by collection-NSOM)
Intensity statistics,
Observables
2D Spatial autocorrelation function of intensity profiles,
Speckle grain size
(Gaussian fitted FWHM of autocorrelation function )
1 um
154.6 nm
1 um
0
5
10
15
20
25
0
500
1000
0
5
10
15
20
25
0
1000
500
Frequency
Photon counts
Frequency
Photon counts
149.4 nm
1 um
141.9 nm
0
5
10
15
20
25
0
500
1000
Frequency
Photon counts

## Slide 4
a
Translated diffuser
532 nm laser
Lens
Mirror
Mirror
Objective
lens
Lens
Lens
Filter
Filter
Signal
Speckle pattern
EMCCD
Illumination objective
Detection objective
Sample
Illumination
Turbid medium
Detection
(Mid-point) Spurious correlation
Dynamic near-field
speckle illumination
Dynamic far-field
speckle illumination
(Right emitter)
(Left emitter)
(Mid-point) Reduced correlation
(Right emitter)
(Left emitter)
a
b
SOFI
SOFI
Unresolved
Super-resolved
Diffraction-limited (unresolved)
Diffraction-limited (unresolved)
Two fluctuated fluorophores
c
d
Time
Translated diffuser
Translated diffuser
Far-field speckles ]
Disordered medium
Near-field speckles
]
Sample plane
z
Disordered medium
z
Fluorophores

## Slide 5
Fig. 2 Dynamic near-field speckle illumination for NS-SOFI imaging experiment. a Experimental setup with sample-mounting configuration for NS-SOFI imaging experiment. b Schmatic representation of illumination optics in a to produce dynamic near-field speckle illumination. A pair of red and blue sphere describes two independent fluorophores separated within subdiffraction distance under dynamic near-field speckle illumination. c Pictorial description of two-step scattering of a laser beam through the translated diffuser and turbid medium, which results in dynamic near-field speckle illumination at the sample plane.
b
a
c
Time
Translated diffuser
Translated diffuser
Far-field speckles ]
Turbid medium
Near-field speckles
]
Two fluctuated fluorophores
Sample plane
z
Turbid medium
Translated diffuser
532 nm laser
Lens
Mirror
Mirror
Objective
lens
Lens
Lens
Filter
Filter
Signal
Speckle pattern
EMCCD
Illumination objective
Detection objective
Sample
z
Illumination
Turbid medium
Fluorophores
Detection

## Slide 6
Fig. 3 Effect of subwavelength grain size of near-field speckle patterns on fluorescence fluctuation of two adjacent fluorophores. a,b Two independent fluorophores (depicted as a red and blue sphere for a clear distinction) are assumed to be separated within subdiffraction distance under dynamic speckle illumination in the far- (a) and near-field (b). Examples of fluorescence intensity fluctuation trace measured during 100 frames of dynamic speckle illumination sampled at the locations of the two fluorophores and their midpoint. In contrast to far-field speckles (a), dynamic near-field speckle illumination (b) of subwavelength grain size produces independent fluctuation of two fluorophores favorable for SOFI processing. Here, the transparent Gaussian lobes assigned to each fluorophore represent the scale of the point spread functions of the base fluorescence detection imaging system.
Time
Time
a
b
Spurious correlation
Vanishing correlation
Near-field
speckle illumination
Far-field
speckle illumination
: Two independent fluorophores separated within subdiffraction distance

## Slide 7
Time
Time
a
b
Spurious correlation
Vanishing correlation
Near-field
speckle illumination
Far-field
speckle illumination
: Two independent fluorophores separated within subdiffraction distance

## Slide 8
Fig. 1 Comparison of speckle patterns in the far- and near-field. a Diagrams comparing far-field and near-field speckle patterns. In contrast to far-field speckle patterns having propagated over a distance longer than a wavelength (z ≫ λ), near-field speckle patterns occur within a subwavelength (z < λ) of the exit surface of a turbid medium, preserving evanescent high spatial-frequency Fourier components. b,c Measured intensity profiles of speckle patterns in the far-field (b) and the near-field (c). Color bars express normalized intensity. d A cross-sectional line profile along the dashed white line in the spatial autocorrelation image (inset) of the near-field speckle pattern (c).
0
1
z
y
x
Turbid medium
a
Far-field speckle pattern
d
Near-field speckle pattern
z < l
z >> l
c
500 nm
b
Incident Laser beam
0
0.5
1.0
1.5
0
2.0
-0.5
-1.0
-1.5
-2.0
FWHM = 150 nm
0
0.2
0.4
0.6
0.8
1.0
1.2
Distance (µm)
Normalized Intensity (a.u.)

## Slide 9
Fig. 4 NS-SOFI resolution gain tested by computational test targets. a Two diverging filaments as the ground truth for our computational resolution test. b Mean image of the speckle-fluctuated image stack equivalent to a wide-field diffraction-limited image under uniform illumination. c The second order S-SOFI images under far-field (left, 2nd S-SOFI) and near-field (right, 2nd NS-SOFI) speckle illumination. d Third-order S-SOFI images under far-field (left, 3rd S-SOFI) and near-field (right, 3rd NS-SOFI) speckle illumination. e Cross-sectional intensity profiles along linecuts over the mean image (b), 2nd S-SOFI image (c, left), and 2nd NS-SOFI image (c, right). f Cross-sectional intensity profiles along linecuts over the mean image (b), 3rd S-SOFI image (d, left), and 3rd NS-SOFI image (d, right). Scale bars: a-d 300 nm
Object
Mean
2nd S-SOFI
3rd S-SOFI
2nd NS-SOFI
3rd NS-SOFI
0
1
a
b
c
d
-0.3
-0.1
0.1
0.3
0
0.2
0.4
0.6
0.8
1
1.2
-0.3
-0.1
0.1
0.3
0
0.2
0.4
0.6
0.8
1
1.2
Distance (µm)
Normalized Intensity (a.u.)
Distance (µm)
e
f
150 nm
160 nm
280 nm
280 nm
160 nm
100 nm
Mean
2nd S-SOFI
2nd NS-SOFI
Mean
3rd S-SOFI
3rd NS-SOFI
Normalized Intensity (a.u.)
-0.2
0
0.2
-0.2
0
0.2

## Slide 10
Object
Mean
2nd S-SOFI
3rd S-SOFI
2nd NS-SOFI
3rd NS-SOFI
0
1
a
b
c
d
-0.3
-0.1
0.1
0.3
0
0.2
0.4
0.6
0.8
1
1.2
-0.3
-0.1
0.1
0.3
0
0.2
0.4
0.6
0.8
1
1.2
Distance (µm)
Normalized Intensity (a.u.)
Distance (µm)
e
f
150 nm
160 nm
280 nm
280 nm
160 nm
100 nm
Mean
2nd S-SOFI
2nd NS-SOFI
Mean
3rd S-SOFI
3rd NS-SOFI
Normalized Intensity (a.u.)
-0.2
0
0.2
-0.2
0
0.2

## Slide 11
2
3
732±40 nm
315±10 nm
c
Distance (µm)
Mean (line 1-17)
Mean (line 18-45)
2nd NS-SOFI (line 18-45)
3rd NS-SOFI (line 18-45)
1
4
3
20
30
20
324±5 nm
1
4
3
44
17
16
a
b
e
742±5 nm
34
33
SEM
1
16
44
17
44
17
44
17
0
1
2
3
4
5
6
7
8
9
10
11
0.0
0.5
1.0
0.0
0.5
1.0
0.0
0.5
1.0
0.0
0.5
1.0
44
34
33
1
Normalized Intensity (a.u.)
Mean
3rd NS-SOFI
2nd NS-SOFI
2
3
4
4
3
Mean (line 1-16)
Distance (µm)
Mean (line 17-44)
2nd NS-SOFI (line 17-44)
3rd NS-SOFI (line 17-44)
315±10 nm
732±40 nm
33
34
27
28
27
28
4
3
1
2
3
4
c
d
27
28
375±5 nm
Fig. 5 Experimental test of resolution enhancement with NS-SOFI technique. a SEM image of a ruler pattern milled on 30 nm-thick gold layer deposited on top of a coverslip. Each line dip is labeled with fluorescent colloidal quantum dots to provide a reference length for fluorescence imaging system under test. Total of 44 lines are numbered as indicators of the individual lines. b A diffraction-limited mean image is defined as the average of a set of fluorescent images acquired under dynamic near-field speckle patterns. c,d 2nd and 3rd NS-SOFI images of the fluorescent line arrays in the second row (from line 17 to 44). e Cross-sectional intensity profiles taken over the mean (b), 2nd and 3rd NS-SOFI images (c,d). More than 20 intensity profiles are taken in parallel to the dashed lines (-purple, -black, -blue, and -red) and then averaged to produce a single representative intensity profile as shown in e, from which the lateral spatial resolution of each fluorescent image is measured. Scale bars: a-d 1 mm.

## Slide 12
324±5 nm
1
4
3
44
17
16
a
b
e
742±5 nm
34
33
SEM
1
16
44
17
44
17
44
17
0
1
2
3
4
5
6
7
8
9
10
11
0.0
0.5
1.0
0.0
0.5
1.0
0.0
0.5
1.0
0.0
0.5
1.0
44
34
33
1
Normalized Intensity (a.u.)
Mean
3rd NS-SOFI
2nd NS-SOFI
2
3
4
4
3
Mean (line 1-16)
Distance (µm)
Mean (line 17-44)
2nd NS-SOFI (line 17-44)
3rd NS-SOFI (line 17-44)
315±10 nm
732±40 nm
33
34
27
28
27
28
4
3
1
2
3
4
c
d
27
28
375±5 nm

## Slide 13
Fig. 6 Resolution enhancement with NS-SOFI technique using fluorescent beads with emission wavelengths of 560 nm. a Mean (diffraction-limited resolution), b 2nd NS-SOFI and c 3rd NS-SOFI super-resolution images of the same region of interest. Intensity profiles are taken along the dashed lines in each image to compare the resolution. d SEM image of the true location of fluorescent beads in the same field-of-view of optical images (a-c). The white arrows indicate the corresponding positions of the beads in the 3rd NS-SOFI image. e Three intensity profiles taken along the dashed lines in optical images (a-c). Fluorescent beads separated by 175 nm are resolved by third order NS-SOFI processing (solid red lines in e). Scale bars: a-d 500 nm
3rd NS-SOFI
Distance (µm)
Normalized Intensity (a.u.)
Mean
2nd NS-SOFI
3rd NS-SOFI
2nd NS-SOFI
Mean
SEM
175 nm
0
0.1
0.2
0.3
-0.1
-0.2
-0.3
a
b
c
d
e
175 nm

## Slide 14
3rd NS-SOFI
Distance (µm)
Normalized Intensity (a.u.)
Mean
2nd NS-SOFI
3rd NS-SOFI
2nd NS-SOFI
Mean
SEM
175 nm
0
0.1
0.2
0.3
-0.1
-0.2
-0.3
a
b
c
d
e
175 nm

## Slide 15
Figure S1. Sample information for figure 5, 6.
Coverslip
Au
Au
QDs
35 nm
Au
Unwanted FIB dip
150 nm
5 nm Cr
Au
Unwanted void
c
Pattern transferred on the Au film
Line patterns as input to focused-ion beam
b
30 nm Au thin film
CdSe quantum dots
Coverslip
Coverslip
Coverslip
a
Spray coating
a white turbid layer
c
Fig. S1 Schematics of sample preparation process. a Preparation of turbid media to generate near-field speckle patterns at the sample plane. Several trials of spray coating a bare coverslip with a white paint layer composed of TiO2 nanoparticles and fixative polymer easily create a few micrometer-thick turbid medium to ensure multiple scattering of incident laser beam. b Three steps to fabricate the fluorescent length standard specimen in Fig. 5. c Dry-casting diluted fluorescent beads for the specimen in Fig. 6.

## Slide 16
b
30 nm Au thin film
CdSe quantum dots
Coverslip
Coverslip
Coverslip
a
Spray coating
a white turbid layer
c

## Slide 17
Figure S2. Lateral spatial resolution : Dip visibility
Fig. S2 Definition of lateral spatial resolution and resolution gain used throughout this paper, particularly in Figs. 5 and 6. a An example set of ground truth template, mean (diffraction-limited resolution), and third-order NS-SOFI image (super-resolution third NS-SOFI) generated as shown in Fig. 5. All scale bars represent 500 nm. b An example of a two-peak cross-sectional intensity profile taken over the third NS-SOFI image. By taking intensity values (I1,max and I2,max) at each peak and the dip (Imin), we compute the average visibility of the two emitters considering their asymmetric intensity (definition below). The spacing d between two emitters at which dip visibility becomes 0.1 is defined as the lateral spatial resolution of the image. c All three projected intensity profiles taken from mean and third NS-SOFI images (a) have the same dip visibility of 0.1, so d1 is the diffraction-limited resolution, and d2 represents the resolution of the super-resolution third NS-SOFI image. The resolution gain of the third NS-SOFI image is defined as the ratio expressing (d2/d1)-fold enhancement.
b
Truth
Mean
FS-SOFI2
NS-SOFI3
0
A
B
C
a
1
0
0.2
0.4
0.6
0.8
1.0
0
0.2
0.4
0.6
0.8
1
Distance ()
Linecut A
Linecut B
Linecut C
1.2
Normalized Intensity
c
Normalized Intensity
Distance ()
Linecut C
Resolution gain =

## Slide 18
b
Truth
Mean
FS-SOFI2
NS-SOFI3
0
A
B
C
a
1
0
0.2
0.4
0.6
0.8
1.0
0
0.2
0.4
0.6
0.8
1
Distance ()
Linecut A
Linecut B
Linecut C
1.2
Normalized Intensity
c
Normalized Intensity
Distance ()
Linecut C
Resolution gain =

## Slide 19
Figure S3. Simulating dynamic near-field speckle patterns
0
1
Fully-developed speckle
A speckle pattern of the grain size
a
b
c
Far-field speckles
Near-field speckles

## Slide 20
0
1
Fully-developed speckle
A speckle pattern of the grain size
a
b
c
Far-field speckles
Near-field speckles

## Slide 21
Intensity average
SOFI processing
2nd NS-SOFI (raw)
3rd NS-SOFI (raw)
2nd NS-SOFI (dec)
3rd NS-SOFI (dec)
2nd NS-SOFI (FRW)
3rd NS-SOFI (FRW)
Lucy-Richardson deconvolution
Fourier-reweighting
(with typ. 3,000 frames)
Figure S4. Workflow of NS-SOFI processing

## Slide 22
Intensity average
SOFI processing
2nd NS-SOFI (raw)
3rd NS-SOFI (raw)
2nd NS-SOFI (dec)
3rd NS-SOFI (dec)
2nd NS-SOFI (FRW)
3rd NS-SOFI (FRW)
Lucy-Richardson deconvolution
Fourier-reweighting
(with typ. 3,000 frames)